## Slide 1: Thermo Mechanical Modeling of Continuous Casting with Artificial Neural Network
Tadej Kodelja
COBIK, Solkan, Slovenia
Supervisor
Prof.dr. B Šarler

## Slide 2: Scope
Continuous casting of steel and its physics
Approximative numerical models based on artificial neural network (ANN)
Modelling of continuous casting of steel by ANN
Conclusions and future work

## Slide 3: Goals
Introduction to steel process modelling
Introduction and motivation for ANN modelling
Assessment of physical and ANN modelling of continuous casting of steel

## Slide 4: Steel Production Process Path

## Slide 5: Steel Production Simulation Scheme
Final Measured Material Properties
Elongation (A)
Tensile strength (Rm)
Yield stress (Rp)
Hardness after rolling (HB)
Necking (Z)

## Slide 6: Continuous Casting of Steel
Process was developed in the 1950s
The most common process for production of steel
90% of all steel grades are produced by this technique
Types
  Vertical, horizontal, curved, strip casting
Typical products
  Billets, blooms, slab, strip

## Slide 7: Continuous Casting of Steel

## Slide 8: Characteristic Regimes in a Solidifying Continuous Casting
Regimes
  LIQUID (liquid, particles, inclusions,…)
  SLURRY (equiaxed dendrites + liquid)
  POROUS (columnar dendrites + liquid)
  SOLID (dendrites)

## Slide 9: Numerical models of the Continuous Casting
Thermal models
  Describes heat transfer with solidification
  Casting velocity is constant for all phases
  Using slice model
Fluid models
  Turbulent fluid flow on a fixed geometry
  Modeling of the turbulent flow involves solving additional two transport equations
Thermo-fluid models
  Involves the solution of the fluid flow with the heat transfer, solidification and species transport
  Much more complex to numerically implement

## Slide 10: Slice Model
Slice traveling schematics in the billet
  Fast calculation time
  x-y cross sectional slide is moving from top horizontal to bottom vertical position
  Temperature and boundary condition are assumed as time dependent
Notes: Temperature and boundary conditions are assumed as time dependant based on constant speed and position of the slice

## Slide 11: Macroscopic Transport Model
Governing equations
  Enthalpy transport
  Mixture and phase enthalpies
  Solved based on initial and boundary conditions that relate the enthalpy transport with the process parameters
28 x 28 points
Notes: The boundary temperature of the slice is defined by Heat tansfer coefficient and temperature of cooling fluid
The energy ballance is

## Slide 12: Example of CC Simulation

## Slide 13: Artificial Neural Network

## Slide 14: Artificial Neural Network - ANN
An information-processing system that has certain performance characteristic similar to biological neural networks
Have been developed as generalizations of mathematical models of human cognition
  Information processing occurs at many simple elements called neurons
  Signals are passed between neurons over connection links
  Each link has an associated weight
  Each neuron applies an activation function

## Slide 15: ANN - Types
Feedforward NN
Feedforward backporpagation NN
Self organizing map (SOM)
Hopfield NN
Recurrent NN
Modular NN
…

## Slide 16: ANN – Examples of Applications
Is an extremely interdisciplinary field
Signal processing
  Suppressing noise on a telephone line
Control
  Provide steering direction to a trailer truck attempting to back up to a loading dock
Pattern recognition
  Recognition of handwritten characters
Medicine
  Diagnosis and treatment
Speech production / recognition, business…
Notes: Fundamentals of neural networks. Str. 7-11

## Slide 17: ANN - Characterization
Architecture - pattern of connections between the neurons
Training or learning – method of determining the weights on the connections
Activation function
Input
units
Hidden
units
Output
units
Notes: Fundamentals of neural networks. Str. 3-5

## Slide 18: ANN - Architecture
The arrangement of neurons into layers and the connection patterns between layers
Single-layer net
  Input and output units
Multi-layer net
  Input, output and hidden units
Competitive layer
Notes: Fundamentals of neural networks. Str.12-14

## Slide 19: ANN – Training or Learning
Supervised learning
(error based)
Reinforcement learning
(output based)
Unsupervised learning
Hebbian
Competitive
Stochastics
Error correction
Gradient descent
Least mean square
Back propagation
Learning algorithms
Notes: 08-Neural network s str. 25
Supervised learning is based on input and output data. Learning process is based on comaparison on
Unsupervised learning is based on input data. The system learns on its own, by discovering the structural features in the inputs patterns.

## Slide 20: ANN – Activation Functions
Typically, the same activation function is used for all neurons in any particular level
Identity function
Binary step function
Binary sigmoid
Bipolar sigmoid
Hyperbolic tangent
Notes: Fundamentals of neural networks. Str. 17-19

## Slide 21: ANN – Feedforward Backpropagation
A gradient descent method to minimize the total squared error of the output
A backpropagation (multilayer, feedforward, trained by backpropagation) can be used to solve problems in many areas
The training involves three stages
  The feedforward of the input training pattern
  The calculation and backpropagation of the associated error
  The adjustment of the weights
Feedforward
Backpropagation
Update weights

## Slide 22: ANN –Backpropagation Algorithm

## Slide 23: ANN –Backpropagation Algorithm
Feedforward
Step 3
Each input unit receives input signal and broadcasts the signal to all units in the layer above (hidden layer)
Step 4
Each hidden unit
sums its weighted input signals
applies its activation function
and sends this signals to all units in the layer above (output unit)
Step 5
Each output unit
sums its weighted input signals
and applies its activation function

## Slide 24: ANN –Backpropagation Algorithm
Feedforward
X1
X2
Xn
Z1
Zj
Y1
Yk
Weights
Input
Sums weighted IN signal
Apply activation function
Weights
Sums weighted IN signal
Apply activation function

## Slide 25: ANN –Backpropagation Algorithm
Backpropagation of errors
Step 6
Each output unit receives a target pattern
computes its error information term
calculates its weight correction term
calculates its bias correction term
and sends to units in the layer below
Step 7
Each hidden unit sums its delta inputs
calculates its error correction term
calculates its weight correction term
and calculates its bias correction term

## Slide 26: ANN –Backpropagation Algorithm
Backpropagation of errors
X1
X2
Xn
Z1
Zj
Y1
Yk
Weights
Input
Weight correction term
Weights
Output
Error information term
Bias correction
term
Delta inputs
Error information term
Weight correction term
Bias correction term

## Slide 27: ANN –Backpropagation Algorithm
Update weights and biases
Step 8
Each output unit updates its bias and weights
Each hidden unit updates its bias and weights

## Slide 28: ANN – Training-Data
Training-data quality
Sufficient number of
training data pairs
Training data points distribution
Verification points selection

## Slide 29: ANN – Calculation of response
After training, a backpropagation NN is using only the feedforward phase of the training algorithm
Step1
  Initialize weights
Step2
  For set activation of input unit
Step3
  For
Step4
  For

## Slide 30: Modeling of continuous casting of steel by ANN

## Slide 31: Physical Simulator Parameters
21 Input parameters
  Charge number
  Steel type
  Concentration: Cr, Cu, Mn, Mo, Ni, Si, V, C, P, S
  Billet dimension
  Casting temperature
  Casting speed
  Delta temperature
  Cooling flow rate in the mold
  Cooling water temperature in sprays
  Cooling flow rate in wreath spray system
  Cooling flow rate in 1st spray system
21 Output parameters
  ML
  DS
  T

## Slide 32: Generating Parameters & Outputs
JMatPro
Training Data Generator
Input parametrs
Input parametrs
Input parametrs
Physical symulator
Physical symulator
Physical symulator
Training data file
. . .
. . .
Node 1
Node 2
Node i

## Slide 33: Casting Parameters & Outputs
ID | Name & units | Description | Range in the training set
1 | Tcast [oC] | Casting temperature | 1515 - 1562
2 | v [m/min] | Casting speed | 1.03 - 1.86
3 | DTmold [oC] | Temperature difference of cooling water in the mold | 5 - 10
4 | Qmold [l/min] | Cooling flow rate in the mold | 1050 - 1446
5 | Qwreath [l/min] | Cooling flow rate in wreath spray system | 10 - 39
6 | Qsistem1 [l/min] | Cooling flow rate in 1st spray system | 28 - 75
ID | Name & units | Description & units | Range in the training set
1 | ML [m] | Metallurgical length | 8.6399 - 12.54
2 | DS [m] | Shell thickness at the end of the mold | 0.0058875 - 0.0210225
3 | T [oC] | Billet surface temperature at straightening start position | 1064.5 - 1163.5

## Slide 34: Casting Parameters & Outputs

## Slide 35: Training the ANN
NeuronDotNet open source library
200000 total IO pairs
  100000 training IO pairs
  100000 verification IO pairs
Settings for ANN
  Epochs 50000
  Hidden layers 1
  Neurons in hidden layer 25
  Learning rate = 0.3
  Momentum = 0.6

## Slide 36: Training the ANN
RMS errors during training

## Slide 37: Studies
Relations between training time, training data and errors

## Slide 38: Study of Errors
Relative errors in verification points

## Slide 39: Parametric Studies
Response around Points on a Line Between Two Points

## Slide 40: Studiy: Uniformity of Training Points Distribution
Euclidean distances to the N-th point
Closest point
9-th closest point

## Slide 41: Conclusions and future work
Dedicated SW framework was developed
Studies to examine the accuracy of ANN based on physical model
ANN approximation is much faster than physical simulation
Complementing physical models with ANNs
Replacing physical models with ANNs
Upgrading of the ANN model for continuous casting with the model of the whole production chain
Development of new methods for checking the quality of training-data
Notes: Conclusion in the article

## Slide 42: References
ŠARLER, Božidar, VERTNIK, Robert, ŠALETIĆ, Simo, MANOJLOVIĆ, Gojko, CESAR, Janko. Application of continuous casting simulation at Štore Steel. Berg- Huettenmaenn. Monatsh., 2005, jg. 150, hft. 9, str. 300-306. [COBISS.SI-ID 418811]
Fausett L.. Fundamentals of neural networks: architectures, algorithms and applications. . Englewood Cliffs, NJ: Prentice-Hall International, 1994.
I. Grešovnik, T. Kodelja, R. Vertnik and B. Šarler: A software Framework for Optimization Parameters in Material Production. Applied Mechanics and Materials, Vols. 101-102, pp. 838-841. Trans Tech Publications, Switzerland, 2012.
I. Grešovnik: IGLib.NET library, http://www2.arnes.si/~ljc3m2/igor/iglib/.
Acknowledements
Prof.dr.Božidar Šarler, dr. Igor Grešovnik, dr. Robert Vertnik
Notes: Conclusion in the article

## Slide 43: Thank you!